LEDs do not require hermetic packaging, or do they?

# Felipe Rudge Barbosa and Edson Moschim

## Laboratório de Tecnologia Fotônica - LTF, FEEC-Unicamp,

## Av. Albert Einstein 400, Campinas SP, 13083-970, Brazil

Rudge;moschim@dsif.fee.unicamp.br

### ABSTRACT

It is a critical issue in many applications that high-performance and high-power Leds have hermetic packaging; however, indoor or environment-protected applications, non-hermetic packaging will suffice. We have developed, tested and analyzed several Led configurations and packaging structures. Decision for specific devices and packages has to be driven by the final application. Detailed construction and operation are considered for different applications.

### INTRODUCTION

Light emitting diodes have been around for over 100 years [ref.1], however their modern versions are fruit of the fantastic development of semiconductor laser diodes in the last 50 years, [ref.2]. It is well-known that all practical applications of these devices, both lasers and Leds, require careful packaging. Whether to choose hermetic – more reliable and more costly – or non-hermetic –more straightfor-ward and much less costly – remains an open question that specific applications will answer. However, new packaging technologies and materials can establish new areas, and a cost efficient analysis might play an important role.

### HERMETIC and NON-HERMETIC PACKAGING

Packaging of semiconductor devices is defined as the proper encapsulation of chips, either single or integrated devices, in order to preserve their dynamic characteristics in different environments. These characteristics involve electrical and thermal conditions, as well mechanical and chemical. Harsh environments are those exposed to variable atmospheric conditions, to mechanical vibrations, to electrical transients, sparks and static discharges; and to strong thermal variations. On the other hand, less demanding applications are home appliances, indoor TVs and displays; intra-building (in-premises) communications and control. Therefore the packaging of these devices, in this specific case optoelectronic components, whether hermetic (metal-ceramic) or non-hermetic (plastic) is primarily decided by the final application, but it must also comply with the device characteristics and operating conditions. All this may sound a bit obvious, but in many cases a specific choice may be difficult to combine and balance cost, performance and reliability. Furthermore, as previously mentioned, new materials and processes start to mix and match various packaging technologies, making choices more complex but more flexible.

Fig. 1 – Hermetic and non-hermetic packaging .

Hermetic packaging is by definition an encapsulation process that allows no gas or liquid interaction with the inside of the package, and this must remain so for the lifetime of the device, which can easily exceed 10 or 15 years. On the other hand, thermal dissipation must be very good (better than 0.2 cal/cm.s.K); electrical contacts obviously perfect; and compliance with thermal and mechanical stability and shock/vibration resistance. To accomplish these features only metallic and ceramic/glass packages are eligible; also, on the inside, no epoxy or any plastic or low-gassing glue should be present; only glass, ceramics, metals, and of course, semiconductors.

Non-hermetic packaging, on the other hand, is free to use any materiasl, in any combination, abiding only to device integrity and minimal protection to shockh and environment. Ceramic subtrates and metallic pads and contacts are used, but encapsulation itself is invariably acrylate or silicone.

### LED PACKAGING

Today, the packaging of semiconductor Leds still follows the above rules, but the mixing of technologies, such as advanced ceramics (AlN and Al2O3) and thermo-plastics, as well as pad and trail lithography will be suppling the needs of high power devices, for IR, visible and UV-blue applications.

Fig. 2 shows a high power device encapsulation, with a ceramic-metallic base for efficient heat dissipation; and a glass dome for high luminous throughput and hermetic sealing.

Fig.2 – High-power hermetic Led array [ref.3].

Interesting is the fact that in automotive and aeronautical (embarked) applications, devices are mostly in protected surroundings, thus packaging need not be perfectly hermetic, but just moisture resistant.

The device in Fig. 4 is a 16-chip array, on Au-Ni pads over alumina; the sealing is solely silicone; a cutaway view can be seen in Fig. 5, glass dome is not present. Notice however in fig.4 that the silicone sheet with lens covers the whole alumina substrate; this way it gets very much resistant to moisture and vapour (but not to liquids).

Fig.4 – Non- hermetic Led array [ref.6] .

Fig.5 – Cut-away view of above; the chips and particules are due to the cutting [ref.8] .

Multichip encapsulation allows for colored (RGB-W) devices for demanding applications such as outdoor high-luminosity solutions for architectural purposes. (Fig.3).

Fig.3 – RGB-W Led-lit roof-cover structure [ref.3]  .

### LED Materials and Interfaces

It should be noted that a critical point in device reliability and durability are the metal-semiconductor and metal-ceramic interfaces. These must show always low thermal resistance, low electrical resistance, and long term stability. In the next section we present data and discuss these parameters.

To properly locate the typical semiconductor materials and their wavelength ranges, we will list some of the most relevant, with just active region/substrate denominations. Red and very-near-IR (620 to 850 nm): GaAlAs/ GaAs; near-IR (1300-1600nm) InGaAsP/InP; blue-green InAlAs/GaN/sapphire (300-540nm). These different material combinations may – and invariably do – cause stresses in the active materials and their interfaces.

. .

Fig.6 – Edge-emitting device soldered onto metallized-Si heat dissipator [ref.7]

Beyond the chip internal stresses, carefully calculated to meet device durability and stability, care must be taken on the p and n metallizations to avoid additional stress and provide excellent contact and thermal conductivity.

Typical p-contact is bottom-up CrAl-CrAu-Au; and n-contact is Ni-Sn-Au; many other combinations may apply, including zinc (Zn) and titanium (Ti); invariably surface metal on both sides is Au for optoelectronic devices.

Die-attach is also very critical and is ruled by the substrate and the built-in stresess of the chip. The GaAlAs/GAAs devices are very sensitive to thermal expansion stresses, therefore lower temperature soldering with more ductile metals is necessary (In-alloys); on the other hand, the sapphire substrate is a very hard material which will withstand harder and very stable alloys with higher eutectic-point temperatures (AuSn and AuSi). In the following some materials and alloys.

Die-attach: In, 156 C; SnAgCu-SAC, 217 C; AuSn, 280 C; over Si, Cu, Al, alumina; depends on device/die (single chip, IC, opto/micro), application and requirements;

Mounting – package assembly (metallic/ ceramic);; InSn 118(C; InPbAg, 142(C.

### LED Electro-Optic Characteristics

The main purpose of packaging is preserving all the characteristics of the packaged devices, for the longest period of time, and under the most varied conditions.

Light-current and voltage current in the pulsed and continuous modes are stablished at devices initial life, after die-attach for heat dissipation. The difference between curves in pulsed and cw is a measure of the heat resistance of device; for good, reliable devices it must be small. Notice that diode lasers and Leds are current devices, and above the diode fwd-threshold (shoulder) voltage (below 5V from IR to UV devices) the VxI curve remains almost constant. it is usual (especially for displays) to assemble Leds in series, with a common current drive.

Fig.7 – Electro-optic characteristics from an Eled.

Further characterizations include spectra and beam-quality, which must also be preserved.

One must establish these original conditions and verify their maintenance through accelerated tests in which high-current-induced and temperature-induced stresses, which are the reveleant parameters are combined to investigate device failure; from those one may ensure, but not guarantee, device presumed lifetime.

Fig.7 – Characteristic emission of high-power white Led arrays. Notice the series connection.

### CONCLUSION

LED devices have been established for several decades as a key technology in generating cold and intense light from optoelectronic diode emitters, They share construction and assembly technologies with diode lasers, but they are simpler and more reliable and durable devices, with less stringent requierements of packaging and operation.

It is a critical issue in many applications that high-performance and high-power Leds have hermetic packaging, whereas, indoor or environment-protected applications, non-hermetic packaging will suffice. We have developed, tested and analysed several Led configurations and packaging structures. The decision for specific devices and packages has to be driven by the final application.

Finally, R&D and innovation in the optoelectronic technology has permitted an enormous evolution in the ranges of emitted power and operating wavelengths. And production costs are high, but processes are efficient, and the yield (throughput) is high and device prices get lower; new applications are everywhere today; high-performance and high-power Leds are widely available.

We expect to have contributed to the knowledge and understanding of these fantastic optoelectronic devices.

Authors acknowledge collaboration with the Microelectronic Packaging Division (DEE) of MCT/CTI, Campinas, Brasil.

### REFERENCES

N.Zheludev, “The life and times of the LED — a 100-year history”, Nature Photon.,VOL 1 | APRIL 2007 |

Leds Magaz., “Solid State Lighting (SSL) industry celebrates 50th birthday of visible LED light”; http://ledsmagazine.com/news/9/10/7? – Oct. 2012;

http://www.laserfocusworld.com/display_article/368304/12/TECHN/New-LED-high-color-rendering-index-and-high-efficiency  (2009)

F. Rudge Barbosa, “Desenvolvimento de Diodos Emissores de Luz de Dupla-Heteroestrutura em InGaAsP/InP e GaAlAs/GaAs para Aplicações  em Comunicações Óticas”, Tese Doutorado, FEEC-Unicamp, Brasil, Julho 1992.

Acrych-Seoul, “High-Power ZP-P4 Model-T Rw”,  Augt. 2010.

http://www.philipslumileds.com/products/luxeonk2  (2009)

F. Rudge Barbosa, F. Borin, A. R. Arakaki, J. D. Aguiar, C. Chaves, “A Novel Optical Accelerometer with extended operation range”, Proceed. SPIE Photonics East 2005 – Sensors for Harsh Environments, paper 5998-7, Boston, USA, Oct. 2005.

Eveline Juntunen; VTT Technology, Oulo, Finland; March 2012.